## Slide 1
Damage in Metal Forming
A brief introduction

## Slide 2: Time to change the length scale
Air Bending
DP800
= 1.2
max = 0.41
= 494 MPa
Original State
!
35,000x
= 100 mm
= 50 mm
t = 1.5 mm
< 85 000 voids
 ~ 11 voids/mm³
~ 27,500,000 voids
~ 390 000 voids/mm³
in the forming zone
macroscopic
microscopic
OK
?
?

## Slide 3: Visualization of forming-induced Damage
Punch
Sheet
Die
Void growth during bending
Dunlap et al., GFE, RWTH Aachen
100 µm (magnification: 200x)
Material: DP800

## Slide 4: Failure vs. Damage
What is failure?
10 µm
Material: DP 800
Cracks, failure
Failed part

## Slide 5: Failure vs. Damage
What is damage?
Initial material
Good part
Inhomogeneity
Coalescence
Void
Source: Reusch (2003)
Tensile Load
Load during plastic deformation
10 µm
Material: DP 800
Cracks, failure
Failed part
Material: DP 800
Kusche et al., IMM, RWTH Aachen
Coalescence of voids
Nucleation and growth of voids
5 µm
?
What is failure?
Damage is not a failure.

## Slide 6: What is Damage?
Damage
Process
Property
Duality

## Slide 7: What is Damage? – It‘s a Process
Damage
Process
Property
Material: DP 800
Kusche et al., IMM
5µm
Khazis (2015)
Load during plastic deformation
Damage Evolution encompasses the nucleation, growth and coalescence of voids.
CT-Scan showing voids

## Slide 8: What is Damage? – It‘s a Property
Damage
Process
Property
The Damage Value describes the influence of the product performance.
undamaged
damaged
As a property, damage links the measurable damage values with the degradation of the product performance.

## Slide 9: Conventional Product Development Cycle
Component with unknown safety margin
Material properties
Design
Forming process
Component geometry
Load
Function
Strain hardening

Residual stresses

Damage
X

## Slide 10: Improving the Product Development Cycle
Component with known safety margin / improved product performance
Material properties
Design
Component geometry
Load
Function
Product properties
Damage
Prediction of performance
Strain hardening

Residual stresses

Damage
X
Strain hardening

Residual stresses

Damage

Damage controlled manufacturing
Casting
Forming
Heat treatment
…

## Slide 11: Controlling Damage in Bending
DP800
max = 0.41
= 494 MPa
Air Bending
Damage is controlled via additional counter-pressure on the outside.
t = 1,5 mm
Original State
< 85 000 voids
 ~ 11 voids/mm³
Damage Controlled Bending Process
= 100 mm
= 50 mm
t = 1.5 mm

## Slide 12: Controlling Damage in Bending
Original State
< 85 000 voids
 ~ 11 voids/mm³
~ 15,100,000 voids
 ~ 210 000 voids/mm³
in the forming zone
- 45 %
~ 27,500,000 voids
~ 390 000 voids/mm³
in the forming zone
Damage Controlled Bending Process
Air Bending
DP800
max = 0.41
= 494 MPa
= 100 mm
= 50 mm
t = 1.5 mm
Notes: Qualitative analysis

## Slide 13: Increasing the Product Performance
Impact performance evaluation

## Slide 14: Increasing the Product Performance
+ 19% in performance
Impact performance evaluation
achieved
Improved safety margin
Reduction of sheet thickness
reduced damage value
enables
Notes: Quantitative analysis

## Slide 15: Summary on Damage
How can damage be characterized
Damage is not a failure!
Damage control in metal forming is possible.
?
How can damage be modeled
What is the dependency on plastic deformation
Damage is a process and a property.
Damage influences the product properties and performance.
Notes: Verweis auf 30 / 90min Versionen, da noch viele offene Fragen, insbesondere Begriffsdefinitionen etc.

## Slide 16: Vielen Dank für Ihre Aufmerksamkeit. Thank you for your attention.